## Slide 1: Experimental and numerical study on size effects in Nanoindentation
Presenter: B.Sc. Yao Yao
Supervisors: Univ. Prof. Dr.-Ing. Sebastian Münstermann
Dr. Ude Hangen
M.Sc. Michael Dölz
M.Sc. Wenqi Liu

## Slide 2: Outline
Introduction
Material
Experimental results and discussion
  Load-displacement curves
  Indentation size effects
  Surface topography
Numerical results and discussion
  Parameterization
  Validation of parameters
  Formulation
Conclusions & outlooks

## Slide 3: Introduction - Nanoindentation
Macro Indentation
Nanoindentation
* IEHK, Lecture slides
* Bruker, Introduction of nanoindentation
Brinell
Vickers

## Slide 4: Introduction – Nanoindentation Application
Mechnical properties distribution with nanoindentation
GPa
DP600 Steel
Comparison of hardness maps
with microscopy maps
Hardness difference between
ferrite and martensite
* Bruker, Brochure

## Slide 5
Introduction – Indentation size effect (ISE)
Conical/Pyramid Indenter：
Spherical Indenter：
Smaller is stronger in indentation:
* Chang Qing Sun, Relaxation of the Chemical Bond, 2014
* Tymiak, Acta Materialia, 2001
Notes: traditional material design: heat treatment, mechanical tests, component test to identify the distance between designed and targeted material properties. trial and error
massively spends material, time, energy, and money
Aim: to develop a simulation toolkit for the computer-assisted material design
Toolkit flow
advantages
in order to achieve the whole circle of the toolkit approach, the information flow between multiscale should be build up using a reference material.
Today, my topic is mainly focused on the transition from component level to macroscopic mechanical property profile.

## Slide 6
Introduction – Indentation size effect (ISE)
Plasticity strain gradient / Geometrically necessary dislocation (GND)
* Swadener, Journal of the Mechanics and Physics of Solids, 2002

## Slide 7
Material
Microstructure
AISI 439: a cold-rolled ferritic stainless steel
Composed of ferrite and small volume of carbides
Average grain diameter： 54 μm

## Slide 8
Experiment setup
{111} grain
{100} grain
a/R: Indentation strain (a: contact radius, R: indenter radius)
Constant stain rate of 0.1 s-1
a/R
0.2
0.3
0.4
Indenter radius
1 μm
2 μm
5 μm
20 μm

## Slide 9
Experiment setup
1&2 μm indenter
5&20 μm indenter
Post SPM is performed to find the location of to
find tested grains.
Calibration of system every time when changing
Indenters.
Post imaging after test to obtain surface topography

## Slide 10
Experiment results and discussion
Load-displacement curves of {111} grain with 1 μm indenter

## Slide 11
Experiment results and discussion
Load-displacement curves of {111} grain with 2 μm indenter

## Slide 12
Experiment results and discussion
Load-displacement curves of {111} grain with 5 μm indenter

## Slide 13
Experiment results and discussion
Load-displacement curves of {111} grain with 20 μm indenter

## Slide 14
Experiment results and discussion
Prominent size effect can be observed:
The hardness increases with smaller
Indenter radius
Slight decrease of hardness with increasing contact depth for the same indenter

## Slide 15
Experiment results and discussion
Surface topography and pile-up patterns
1 um indenter 0.4 strain
{100} grain
1 um indenter 0.4 strain
{111} grain
* Xiaoxue Liu, Master thesis

## Slide 16
Numerical setup
Crystal plasticity model:
Dislocation slip based formulations
Initial critical resolved shear strength:
Work hardening parameters: , a ,
Strain rate parameters: , m

## Slide 17
Numerical setup
Nanoindentation models:
Indenter | Total size (μm3) | Diameter of center circle (μm) | Mesh size of center circle (μm)
1 | 20×20×8 | 4 | 0.1
2 | 20×20×8 | 5 | 0.125
5 | 60×60×15 | 12 | 0.3
20 | 60×60×15 | 24 | 0.6

## Slide 18
Numerical results and discussion
Calibration of work hardening parameters:
Parameters | 
, MPa | 240
a | 1.2
, MPa | 550
Parameters | 
 | 240
a | 1.2
 | 550

## Slide 19
Numerical results and discussion
Calibration of :
Indenter | , MPa
1 μm | 165
2 μm | 130
5 μm | 68
20 μm | 62
Indenter | 
1 μm | 165
2 μm | 130
5 μm | 68
20 μm | 62
1 μm
2 μm
5 μm
20 μm

## Slide 20
Numerical results and discussion
Validation of calibrated parameters in {100} grain at 0.2 strain
1 μm
2 μm
5 μm
20 μm

## Slide 21
Numerical results and discussion
The relationship of and R is fitted by a Boltzmann equation.
The suitable for an indenter with radius between 1 and 20 μm could be calculated from the equation.

## Slide 22
Numerical results and discussion
SPM
Simulation
P-H
1 um indenter
0.4 strain
{100} grain
1 um indenter
0.4 strain
{111} grain

## Slide 23
Conclusions and outlook
Experiments on AISI 439
  Size effect is observed when varying indenter radius;
  The hardness decrease with increasing depth for the same indenter;
  The hardness and pile-up are orientation dependent.
Numerical study with CPFEM
  The size effect is well captured by varying ;
  The relationship between and R is given by a Boltzmann equation.
Outlook
  The calibrated parameters should be incorporated into a mesoscale model.
  Nanoindentation with another indenter radius should be performed to validate the expression.
  Non-local CP model should be used for further study.